## Slide 1
Fig. 1. (a) Molecular structure of TA, (b) Digital and (c) SEM images of TA fibers with different magnifications.
(a)
(b)
(c)
Tannic Acid (TA)
Tannic Acid (TA)-Fiber

## Slide 2
Chart: Temperature (ºC)
TA
TA Fiber
Temperature ℃
1000
800
600
400
200
TG %
100.0
80.0
60.0
40.0
20.0
0.0
Crosslinked TA-Ibu Fiber
TA Fiber
Crosslinked TA Fiber
TA-Ibu Fiber
(a)
(b)
1000
1500
2000
2500
3000
3500
4000
Wavenumbers (cm-1)
650
TA
TA Fiber
Crosslinked TA Fiber
TA-Ibu Fiber
Crosslinked TA-Ibu Fiber
(c)
Fig. 2. Thermal degradation profiles (a) TA molecule and TA fiber, and (b) TA-based fibers and (c) FT-IR spectra of TA-based fibers.

## Slide 3
Fig. 3. (a) Degradation of crosslinked and non-crosslinked TA fibers, (b) Ibuprofen release % profile from crosslinked and non-crosslinked TA-Ibu fibers.
Chart: Time (hour)
| 0.5 | 1 | 1.5 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 24 | 48 | 72 | 120
Crosslinked TA-Ibu Fiber | 4.2179 | 9.0268 | 14.011 | 21.4812 | 32.9836 | 47.6249 | 54.984 | 56.2566 | 63.6127 | 65.4458 | 67.3512 | 68.9597 | 73.115 | 79.1599 | 89.8148 | 93.6375 | 96.3911 | 97.5497
Chart: Time (hour)
| 0.5 | 1 | 1.5 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 24 | 48 | 72 | 120 | 168
Crosslinked TA Fiber | 1.3706 | 7.1089 | 11.4602 | 15.8661 | 24.5064 | 33.6935 | 41.7469 | 48.7414 | 53.4504 | 53.6714 | 53.7992 | 55.6334 | 58.1333 | 61.4861 | 73.6203 | 78.6735 | 80.8836 | 82.4103 | 83.1273
Crosslinked TA-Ibu Fiber | 1.1892 | 6.1106 | 9.4445 | 14.368 | 22.9511 | 31.625 | 38.1158 | 39.232 | 41.021 | 46.8383 | 48.8961 | 52.5004 | 59.5478 | 65.8779 | 78.2919 | 85.232 | 90.6061 | 96.4676 | 98.9297
(a)
Ibuprofen
(b)
Chart: Time (minute)
| 0 | 2 | 4 | 6 | 8 | 10
TA Fiber | 0 | 88.6061 | 90.9576 | 93.6364 | 100 | 100
Chart: Time (minute)
| 0 | 1 | 2 | 3 | 4 | 5
TA-Ibu Fiber | 0 | 71.5243 | 76.0646 | 97.6453 | 98.7788 | 100

## Slide 4
Fig. 4. (a) Hemolysis, and (b) blood clotting index of TA-based fibers at different concentrations, the microscope images of (c) crosslinked TA fiber, (d) red blood cells, and (e) red blood cells in the presence of non-crosslinked TA fibers.
Chart: Concentration (mg/mL)
| 0.5 | 1 | 2
TA Fiber | 76.5762 | 53.1942 | 52.5678
Crosslinked TA Fiber | 99.7005 | 72.213 | 67.787
TA-Ibu Fiber | 52.6456 | 39.1348 | 8.6855
Crosslinked TA-Ibu Fiber | 65.99 | 64.2429 | 59.401
Chart: Concentration (mg/mL)
| 0.5 | 1 | 2
TA Fiber | 0.62402 | 1.4353 | 1.1856
Crosslinked TA Fiber | 14.8525 | 16.9549 | 28.959
TA-Ibu Fiber | 0.61038 | 0.71211 | 0.81384
Crosslinked TA-Ibu Fiber | 8.6809 | 15.7511 | 26.7887
(a)
(b)
(c)
(d)
(e)

## Slide 5
S. aureus
E. coli
Gentamicin
TA Fiber
TA
TA-Ibu Fiber
Crosslinked TA Fiber
Crosslinked TA-Ibu Fiber
Fig. 5. Digital camera images of TA and TA-based fibers against S. aureus (gram +) and E. coli (gram -) bacteria [gentamicin was used as a control].